# STRESSTECH

QZ500-4

## OPERATING INSTRUCTIONS AND PARTS LIST

SAFETY INSTRUCTIONS

Always wear protective clothing, including safety glasses and steel toe boots.

Keep work site neat and clean.

Run the secondary cables overhead or clearly mark the area for trip hazards.

Ensure adequate clearance around the area to be heat treated, is free of any material that could be a fire hazard.

Check to be sure the work piece is adequately supported before starting the heat cycle.

Clearly mark the work area to inform others of ongoing heating.

Inform other workers of the heated area and of the heating element tails on the work piece.

Do not operate or use the heat treating equipment, unless you have read and understand the operating manuals that came with your equipment.

Table of Contents

General Information				1

Post Weld Heat Treatment Set-up		2-4

Top Temperature Controller			5

Operating Instructions				6-10

Trouble Shooting					11-12

Service and Maintenance				13

Welding Supply Instructions			14

Parts List						16-19

Wiring Diagrams					20-22

- 1 -

Electrical Specifications:

Input Requirements		 50 amps @ 480v 3ph 100%

Current Capacity (per zone)				300 AMPS DC

80 VOLTS DC

Output Available 		 500 amps @ 80 VDC 100% duty cycle

Physical Dimensions:

Height:		36"

Width:		20"

Length:		31"

Weight:		500 lbs.

General Information:

The STRESSTECH QZ500-4 is a four zone temperature controller which can be operated semi-automatically (auto-ramping up and down, hold at temperature), or manually (manual ramping, no hold temperature). It consists of four 300 amp contactors, 0-2000 deg. F. temperature controllers, percentage timers for controlling the rate of heating and cooling, if desired. The QZ500-4 also has a 0-500 DC ammeter, to aid in monitoring the current supplied to the heating elements being used.

(Each element will use approximately 50 amps @ 80 DC volts.)

The top temperature controller will maintain any selected temperature between ambient and 2000 deg. for as long a period of time required. The controller will control the heating and cooling rate by opening or closing the contactor as needed.

The contactor, normally open, will close providing current to the heating elements up to a maximum of 300 amps, at 80 DC volts.

- 2 -

Post Weld Heat Treatment Set-up:

1.	Prepare thermocouple wire for attachment to work piece:

a) Cut two thermocouple wires 24" or longer (thermocouple

wires should extend beyond insulation).

b) Strip insulation back approximately 1/4" - 3/8" on both

ends of each wire.

c) On one end of each wire, trim lead ends to a fine point

and bend the last 1/8" at a 90 degree angle.

d) On the opposite end of one wire, install a male

thermocouple plug. Yellow wire (+), Red wire (K).

e) Lightly twist the two wires together. The wire without the

plug will be a spare.

2.	Attach the prepared thermocouple wires onto the work piece using the capacitor-discharge spot welder (ZAP GUN). Operating instructions, for attachment of thermocouple wires, are on the inside of the Zapgun lid.

3.	Thermocouples shall be attached in the following minimum location(s):

ON A HORIZONTAL WORK PIECE:

a) Always at the bottom-dead-center.

b) For component diameters 12 inches or more, add a second

thermocouple at the top-dead-center.

c) For component diameters over 24 inches, place

thermocouples at each 90 degree intermediate location.

ON A VERTICAL WORK PIECE:

a) The same number of thermocouples as above shall be

attached, spaced evenly.

4. 	Thermocouples shall be attached in each zone where heaters are separately controlled.

5.	Thermocouples should be placed so that the anticipated coolest and hottest areas within the heating band are monitored.

- 3 -

Post Weld Heat Treatment Set-up Cont:

6.	When the component wall thickness adjacent to the wall vary significantly (such as by the thicker side being more than about 25% or 1/2" greater than the thinner) then:

a) Additional thermocouples shall be attached so that each of

the above required locations have thermocouples close to

the weld, but both on the thin and thick materials that 	  	   will be under the heating band (e.g., for a pipe welded to 	   a heavy valve) and,

b) for even larger thickness differences (such as for a pipe 	   to a very heavy vessel nozzle), even more thermocouples 	         should be attached on the thicker material, at a distance

from the weld equal to about 3 times the wall thickness at         the weld. If such thermocouples are beyond the heating

band, the gradient should be controlled if and as required         by the Specific Project Instructions.

7.	A system shall be established for positive identification of each thermocouple with the location on the work piece. A sketch or written description of thermocouple locations should be made, identifying each thermocouple.

8.	Select the heating element(s) that best cover the area to be heat treated.

9. 	Tape the heating element(s) onto the work piece using fiberglass strapping tape, and then use stainless steel banding to fasten them securely.

10. 	Insulation shall completely cover the heating elements, and extend beyond their edges somewhat. If possible, the insulation should be at least twice as wide as the heating band.

11.	Fasten the insulation securely to the work piece by using tie wire or banding.

12.	Heating element tails should be brought directly out of the insulation, so as not to overheat the connectors.

13.	Connect thermocouple(s), using thermocouple extension leads, to the thermocouple jack strip on control unit. MAKE SURE thermocouples are plugged into proper jacks; i.e., thermocouple #1 on work piece must be connected to thermocouple jack #1, etc.

- 4 -

Post Weld Heat Treatment Set-up Cont:

14. 	Connect heating elements to splitter cables: (figure 1)

a) Heating elements associated with thermocouple zone #1,

must be connected to circuit #1. This sequence follows

through for each zone of control.

b) Connect a tail from each heating element in circuit #1,

to a splitter cable.

c) Connect the other tail from each heating element in

circuit #1, to a different splitter cable.

d) Using 2/0 power cable extension leads, connect the two

splitter cables from circuit #1 to the two corresponding

jacks on the control unit.

e) Repeat steps b-d, if connecting more than

one zone of control.

15.	Using 6 ft. male to male thermocouple jumper wires, you can connect a temperature recorder to the thermocouple jack strip on the control unit.

(figure 1)

- 5 -

TOP TEMPERATURE CONTROLLER

KEY FUNCTIONS AND DISPLAYS:

- 6 -

Operating Instructions:

1.	Be sure the control power switch on the QZ500-4 is in the OFF position.

2. 	Position the unit in desired location and connect a 480 volt, three phase, 60 amp service to the line cord. Service line should have a fused safety disconnect switch on the feeder side. Wire in accordance with all applicable local and national electrical codes. Make sure unit is properly grounded before placing into service.

3.	Connection of 80 vdc power leads: (figure 2)

ZONE #1

a) Connect a lead from the heating elements to the female

cam-lok on the rear of the unit marked "1".

b) To complete the circuit, connect the remaining lead from

the heating elements to the other female cam-lok

marked "1".

4.	Insert the thermocouple lead, from the work piece, into one of the (#1) thermocouple jacks on the rear of the QZ. The second (#1) jack is used for connecting a temperature recorder.(figure 2)

5.	Repeat steps 3 and 4 using Zone #2, 3, or 4 for heating more than one controlled area.

(figure #2)

- 7 -

Operating Instructions Cont:

MANUAL OPERATION

6.   Make sure all the individual heating circuits are off. Turn on the main power and then the control power switch. Set the percentage timers at 50%. (Heating circuits work on a full on or off principal. 50% power is obtained by turning contactors on for half a minute then off for half a minute.)

7. 	Push the auto/manual switch to the manual position. In the manual position only the percentage timers are used, the top temperature controller does not affect the output.

8.   Check the ammeter on front panel. Each circuit is capable of switching 300 amps, but do not exceed 500 amps total for all four zones. Overloading will cause a fuse to blow inside the unit, which could mean losing a heating cycle.

9.   Check the slope of the temperature chart to determine the rate of rise of the temperature and increase or decrease the setting on the percentage timers as needed to maintain proper heating or cooling rate.

- 8 -

Operating Instructions Cont:

AUTO OPERATION

10.	Make sure all the individual heating circuits are off. Turn on the main power and then the control power switch. Set the percentage timers at 0% (while setting the top temperature controllers).

11.	Push the auto/manual switch to the auto position and set the top temperature controller to the desired holding temperature (set value):

a) The controller runs through a self test for about three

seconds and then displays the measured value.

This is called the HOME display.

b) To view the set value, press and release the UP or DOWN

key. The set value will be shown for approximately

2 seconds.

c) To change the set value, press the UP or DOWN key

until the desired soak temperature is displayed. After two

seconds the new value will be accepted and the controller

will return to the HOME display.

12.	Set the top temperature controller to the desired heating ramp rate:

a) Press the SCROLL key twice and an indication of "SPrr"

(set point ramp rate) appears.

b) To view the ramp rate value, press the UP or DOWN key.

The value shown is in degrees per minute.

After two seconds the display will return to "SPrr".

For example,

If you wish to enter a ramp rate of 300 degrees/hour,

you perform the following calculation:

300 degrees/hour divided by 60 minutes = 5 degrees/minute.

c) Change the data indication to the desired ramp rate, using 	   the up and down-keys.

d) The display will return to "SPrr" after two seconds.

e) After 45 seconds the controller will return to the HOME

display. Or you can press the PAGE or SCROLL key once to

return to the HOME display.

- 9 -

Operating Instructions Cont:

13.	Once you have the desired set value, and ramp rate entered into the controller, push the auto/manual switch to the off position.

14.	Turn the percentage timer to 100%.

15.	Push the auto/manual switch to the auto position. This enables the unit to use both the top temperature controller and the percentage timer. In the manual position only the percentage timer is used, the top temperature controller does not affect the output.

16.	The controller will ramp from the present temperature, at the rate you entered into the "SPrr" parameter, to the soak temperature you entered for the set value.

17.	While the controller is ramping, the display may flash "1dLo".

Which is a low deviation alarm, to let you know the work piece is not keeping up with the controller.

18.	The display may also flash "2dHi". Which is a high deviation alarm to let you know the work piece is not keeping up.

19.	The controller will hold the work piece temperature at the set value until you change it to a new value.

20.	At the end of the soak time you will need to change the set point ramp rate "SPrr", if the cooling rate is different than the heating rate. If the rates are the same you won't have to change it.

21.	Once the correct cooling rate is entered into the "SPrr", you will need to change the set value to 0 degrees.

22.	The controller will now ramp from the soak temperature down to 0 degrees.

- 10 -

Operating Instructions Cont:

23.	The weldment area shall be first brought up to about 200 degrees. The temperature recorder shall be checked then for temperature readings of each thermocouple, and for correct chart speed.

24.	During the PWHT cycle, the current should be occasionally checked, especially if any abnormal temperature readings are obtained. A significant drop, such as by the rating of one heater (about 50 amps), would indicate that a heater may be burned out.

25.	At no time shall any two thermocouples, within the heating band, be allowed to differ by more than 150 degrees. If this temperature difference is approached during heating, the heating rate should be slowed.

26. 	Heating shall continue until reaching the holding temperature required by the applicable Welding Procedure.

27.	At the completion of the holding time, begin the cooling.

28.	The power shall not be completely shut off until the temperature cools down to below 600 degrees, unless it is determined by continuous monitoring that the maximum cooling rate will not be exceeded, or that the temperature difference between any two thermocouples will not differ by more than 150 degrees.

29.	Insulation coverings shall not be removed until the temperature drops below 200 degrees, although any stuffed in the ends to fill gaps may be removed if the work piece is in still air and will not exceed the maximum allowable cooling rate.

30.	Check all equipment for damage or wear. Any damaged equipment should be repaired immediately or replaced.

- 11 -

Trouble Shooting:

1.	Temperature does not increase on controller:

a) Check voltmeter on front panel to be sure it is

reading 80 vdc.

b) Percentage timer is turned up to 100%.

c) Check for correct connections of the cables.

d) Check ammeter on front panel. (each heating element

draws approximately 50 amps)

d) Check the set value and set point ramp rate "SPrr"

settings on the controller.

2.	Temperature does not increase on recorder:

a) Check male to male thermocouple wire for a bad

connection at one of the plugs.

3.	Temperature decreases on recorder or controller:

a) The thermocouple wires have been reversed in one of

the plugs. The yellow wire should be in the positive

(+) slot and the red wire in the negative (-) slot.

4.	Contactor chatters:

a) Check the thermocouple connections first. If all the 		   connections are ok, the contactor may be worn out.

5.	Temperature swings when holding at a set point with the top temperature controller:

a) Thermocouples are located too far from heating

elements. The swing can be reduced by turning the

percentage timer down, if the full power is not

needed to maintain the temperature.

6.	Temperature does not stop rising after reaching the set value:

a) Be sure the auto/manual switch is in the auto

position.

- 12 -

Trouble Shooting Cont:

7.	Fault indication on top temperature controller:

a) The controller has a fault indicating function so

that the cause of fault can be removed quickly.

These warn that a fault exists in either the

controller or the connected devices.

INDICATION   :          WHAT  IT  MEANS

1dLo		:		Deviation low alarm

-------------------------------------------------------

2dHi		:		Deviation high alarm

-------------------------------------------------------

S.br		:		Thermocouple sensor break

-------------------------------------------------------

LLLL		:		Out of range low reading

-------------------------------------------------------

HHHH		:		Out of range high reading

-------------------------------------------------------

EE.Er		:

----------------

Err1		:

----------------

Err2		:		Return for repair

----------------

Err3		:

----------------

Err4      :

REPAIR AND CALIBRATION

Due to the nature of its design, if a controller fails to operate correctly consult STRESSTECH. Special equipment is required for calibration and unit MAY have to be returned for repair.

- 13 -

Service And Maintenance:

NEVER work on a unit unless primary power has been disconnected or locked out.

1.	Keep control unit clean and dry.

2.	Periodically check all thermocouple wires and power cables for loose connections or damage. Any damage should be repaired immediately or replaced.

3.	Every six months remove the cover from the unit and, using clean dry air, blow out all dust and dirt from the inside. Do not exceed 25 psi.

4. 	Keep cam-lok connectors clean using scotchbrite pads.

5.	Contactor maintenance:

a) The main contacts should be given regular attention,

especially where heavy loads are involved or a high

number of operations per hour.

b) These contacts are plated with silver cadmium oxide

giving it the same corrosion protection as pure

silver, but greater resistance against contact

welding.

c) Contact surfaces should not be polished or greased.

d) Worn-off contact dust should be carefully brushed

off the insulating parts at each inspection. The de-

ionizing laminations of the arc shield are made of

steel plate to which beads of fused metal may stick

so that the laminations become electrically

connected. If this has occurred, the beads must be

removed by means of a smooth file or suchlike. If

there are layers of sintered contact dust on the

inside of the arc shield, these should also be

scraped off.

e) Change all three contact points if any one becomes

badly worn or pitted.

- 14 -

STRESSTECH  QZ500-4

AS A POWER SOURCE FOR WELDING

To use:

1.  Turn main power on.

2.  Turn control power switch on.

3.  Push auto/manual switch to manual.

4.  Turn percentage timer to 100%.

5.  Plug in cable from welding grid to unit.

(If more than 300 amps is required per welding

station use a "Y" cable between two zones.)

To weld straight polarity:

1.  Connect the male cam-lok from the welding grid to

the negative cam-lok receptacle on the side of the

QZ.

2.  Connect the ground clamp to the work piece and to

the positive cam-lok receptacle of the same zone

on the side of the QZ.

To weld reverse polarity:

1.  Connect the male cam-lok from the welding grid to

the positive cam-lok receptacle on the side of the

QZ.

2.  Connect the ground clamp to the work piece and to

the negative cam-lok receptacle of the same zone on

the side of the QZ.

A second welding grid can be used simultaneously by

connecting it to different zone, providing the same

polarity is used for both welding units.

- 16 -

(figure 1)

- 17 -

Parts List (figure 1):

1.		Voltmeter (0-100vdc)				12005736

2.		Control Power Switch				12008441

ON/OFF Plate					12008460

3.		Main Power Light Assy.

Pilot Lamp Housing				12005231

Pilot Lamp					12005220

Red Lens						12005232

4.		110v. Transformer Fuse Assy.

Fuse Holder					12003930

ABC 15 Amp Fuse				12003947

5.		110v. Outlet Fuse Assy.

Fuse Holder					12003930

AGC 3 Amp Fuse				12003940

6.		Ammeter (0-500amp)				12005721

7.		Contactor Light Assy. (6)

Pilot Lamp Housing				12005231

Pilot Lamp					12005220

Red Lens						12005232

8.		Auto/Manual Switch (6)			12008410

9.		Top Temperature Controller (6)

Eurotherm 2116 Controller		12008645

10.		Percentage Timer Assy. (6)

Aluminum Knob					12009959

Adjusting Pot.				12009984

Solid State Timer				12006702

Dial Plate					12009995

11.		Front panel					12002090A

- 18 -

(figure 2)

- 19 -

Parts List (figure 2):

1.		Rectifier Assembly

2.		Main Transformer				12009350

3.       	500 Amp DC Shunt				12007820

4.		Zone Contactor (4)				12002760

Contactor Bussbar				12001928

5.       	300 Amp Fuse (4)				12003910

6.		Main Transformer				12009350

7.		10” Exhaust Fan					12002226

8.       	Main Contactor					12002765

9.       	480/110v. Transformer			12009331

10.       Panel Mount Cam-lok (8)			12002160

11.		Thermocouple Terminal Strip (2)	12008904

12.		110v. Panel Mount Outlet			12007045

- 20 -

CONTROL DRAWER WIRING DIAGRAM

- 21 –

CONTROL DRAWER WIRING DIAGRAM

- 22 -

BASE UNIT WIRING DIAGRAM

# Text boxes

A Division of Mactech